## Slide 1
Project HYPACT
Cracking of green ammonia to hydrogen ​
using innovative catalyst and adsorbent-assisted plasma technology​
​

## Slide 2: Alternative hydrogen carriers
Compressed hydrogen (C-H2)
Liquid hydrogen (L-H2)
LOHC
  MCH
  (Di)BT
HydroSil
KBH4
Hydrogen derivatives
  Methanol
  methane
Notes: To determine if ammonia is still the best hydrogen carrier an extensive literature study has been composed, investigating several parameters of alternative hydrogen carriers and comparing them with ammonia. The list above were the main competitors.

## Slide 3
Hydrogen Carrier | C-H2 | L-H2 | MCH | DiBT | NH3
Energy consumption conversion to carrier (kWh/kg H2) |  |  |  |  | 
Energy consumption conversion to hydrogen (kWh/kg H2) |  |  |  |  | 
Hydrogen content (kg H2 per m³) |  |  |  |  | 
Purity of H2 after dehydrogenation |  |  |  |  | 
TRL |  |  |  |  | 
Direct use |  |  |  |  | 
Good
Bad
Available hydrogen Carriers
Notes: The main competitors of ammonia are listed again and compared using a colour scale.
The first parameters are the energy consumptipon for the conversion to the carrier and conversion back to hydrogen. These parameters indicate how efficient it is to use this carrier as all energy used for conversion is lost in the end.
The second parameter is the volumetric hydrogen content, indicating how much hydrogen can be stored per cubic meter. The less space the less space needed to store hydrogen the more hydrogen can be carried at a time on a ship.
Next up is the purifty of hydrogen after the dehydrogenation process. This was however not significantly different except for compressed hydrogen as this is 100% hydrogen after decompressing.
The TRL level indicates the entire value chain. Parts of the value chain can be at TRL 9, but if there is a part (like ammonia cracking) that is not at TRL 9, the parameter will not be dark green.
Finaly the direct use of a carrier is also investigated. If a carrier can be used directly it does not require the energy for (de)hydrogenation as well as a purification process afterwards.

## Slide 4: Available hydrogen Carriers
Hydrogen Carrier | C-H2 | L-H2 | MCH | DiBT | NH3
Flammability/ explosiveness |  |  |  |  | 
Toxicity |  |  |  |  | 
Environmental impact |  |  |  |  | 
Health dangers |  |  |  |  | 
Good
Bad
Most toxic/ dangerous for humans
Notes: Safety has also been investigated. Most carriers are very flammable and easy to ignite which can create explosions. Ammonia however is very difficult to ignite so has a low risk for explosiveness. On the other hand it is very toxic and dangerous for human health. The other carriers are less dangerous for humans, but MCH and DiBT are both also toxic.

## Slide 5: HyPACT project scheme
Coordination
(WaterstofNet)

## Slide 6: Project boundary conditions & aims
Boundary conditions
Input: Liquid NH3 at 1 bar
Output: H2 product at 50 bar
Aims
Non-noble abundant metal catalyst
NH3 in H2 product gas < 100 ppb
Target energy cost ≤ 75 kJ.molNH3-1
(x0.09) ≤ 6.94 kWh.kgH2-1
NH3 Conversion ≥ 98%

## Slide 7: Smart heat integration of HyPACT
Plasma heat
Heating reactor
Compression
Energy need
Plasma cracking
Heat recovery
Heat from plasma
Heat from compression
Evaporation of feed
Heating of feed
Heating catalytic reactor
Regeneration of adsorbent
Compression heat
Heating & Evaporation
* Purification has negligible energy cost

## Slide 8: Theoretical energy cost of HyPACT
Chart: Operating pressure (bar)
| 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7 | 7.4999999999999991 | 7.9999999999999991 | 8.5 | 9 | 9.5 | 10
Energy cost | 85.4496 | 81.864 | 79.3848 | 77.498 | 75.9796 | 74.7118 | 73.6253 | 72.6759 | 71.8338 | 71.0776 | 71.1232 | 71.1218 | 71.1884 | 71.3691 | 71.5499 | 71.7307 | 71.9115 | 72.0923 | 72.2731
Plasma | 55 | 55 | 55 | 55 | 55 | 55 | 55 | 55 | 55 | 55 | 55 | 56 | 57 | 57 | 57 | 57 | 57 | 57 | 57
Plasma reactor
Compressor
Compressor
Plasma
5.5 bar
Optimum energy cost & pressure
= 71 kJ.molNH3-1 @ 5.5 bar
Source: own computations
Notes: 6.6 kWh/kgH2

## Slide 9: Project progress second year HyPACT
1. Catalyst development for pre-plasma process (COK-KAT)
2. Plasma reactor (PLASMANT)
3. Thermal swing adsorption (DuEl)
4. Process simulations (COK-KAT)
5. Virtual lab scale demonstration (DuEl)
6. Benchmarking (WaterstofNet)

## Slide 10: 1. Catalyst development for pre-plasma process

## Slide 11
Chart: Temperature [°C]
| 598 | 548 | 498 | 449 | 399 | 349 | 300
5RuAl2O3 | 0.99536 | 0.98886 | 0.87388 | 0.55608 | 0.28187 | 0.17342 | 0.1511
10K5RuAl2O3 - batch 1 | 0.99643 | 0.99489 | 0.99267 | 0.94177 | 0.64736 | 0.3795 | 0.29924
10K5RuAl2O3 - batch 2 | 0.99864 | 0.99776 | 0.99722 | 0.96342 | 0.72889 | 0.42856 | 0.21656
Blank | 0.28581 | 0.16867 | 0.11705 | 0.061855 | 0.027656 | 0.014053 | 0.0094895
Ammonia cracking on Ru catalysts
Conditions: P= 1 atm; NH3 flow rate 40 N mL/min; Wcat= 455 mg; WHSV = 4 h-1, GHSV = 5271 mL g-1 h-1
Ruthenium-based catalyst achieving
conversion > 70% at T < 450°C and a WHSV > 4 h-1
4 h-1 & 99% conversion
≈ 17 kg H2 per kg catalyst per day
Target noble metals:
XNH3 (450°C) > 70%
Ru-alumina
Ru-K-alumina (batch 1)
Ru-K-alumina (batch 2)
Blank

## Slide 12
Chart: T [°C]
| 581 | 535 | 487 | 435 | 390 | 345 | 298
Catalyst 1 | 1.0184 | 1.0132 | 0.90015 | 0.5453 | 0.22908 | 0.085357 | 0.035592
Catalyst 2 | 1.0175 | 1.0064 | 0.81139 | 0.39359 | 0.1492 | 0.053601 | 0.022933
catalyst 3 | 0.95498 | 0.6664 | 0.3307 | 0.14011 | 0.054409 | 0.024246 | 0.015621
Ru-Alumina | 0.99536 | 0.98886 | 0.87388 | 0.55608 | 0.28187 | 0.17342 | 0.1511
Ru-K-Alumina | 0.99864 | 0.99776 | 0.99722 | 0.96342 | 0.72889 | 0.42856 | 0.21656
Development of precious metal-free catalyst
Conditions: P= 1 atm; NH3 flow rate 40 N mL/min; Wcat= 455 mg; WHSV = 4 h-1, GHSV = 5271 mL g-1 h-1
XNH3 (500°C) > 90%
Precious metal-free catalyst achieving
conversion > 50% at T < 500°C and a WHSV > 4 h-1
Target non-noble metals:
XNH3 (500°C) > 50%

## Slide 13
Recap of all self-made catalysts
Chart: NH3 conversion
Conditions: P= 1 atm; T=478°C; NH3 flow rate 40 N mL/min; Wcat= 455 mg; 125-250µm; WHSV = 4 h-1
Top non-noble metal-catalysts achieves target conversion of noble metal catalysts
Non-noble metal
Noble metals
Target conversion non-noble metals
Target conversion noble metals

## Slide 14
Development of precious metal-free catalyst
Influence of pressure on catalyst performance
(max 7 barg in reactor)
Chart: T [°C]
| 581 | 538 | 485 | 439 | 393 | 344 | 298
1 bar | 1.0195 | 1.019 | 1.0179 | 0.98327 | 0.66236 | 0.28745 | 0.10006
7 bar | 1.0129 | 1.0086 | 0.97909 | 0.76878 | 0.42405 | 0.1793 | 0.07195
Conditions: NH3 flow rate 40 N mL/min; Wcat= 455 mg; WHSV = 4 h-1, GHSV = 5271 mL g-1 h-1
Effect of pressure differs between different catalysts
Chart: T [°C]
| 574 | 528 | 482 | 434 | 387 | 342 | 295
1 bar | 0.99255 | 0.96281 | 0.77108 | 0.47641 | 0.24572 | 0.12212 | 0.088004
7 bar | 0.98019 | 0.88524 | 0.64307 | 0.40131 | 0.21204 | 0.11626 | 0.097981
Noble metal catalyst
Δ ≈ 30°C
Non noble metal catalyst
Δ ≈ 20°C

## Slide 15
Long-term stability testing
Conditions: P= 1 atm; NH3 flow rate 40 N mL/min; Wcat= 455 mg; WHSV = 4 h-1, GHSV = 5271 mL g-1 h-1
Chart: Time (day)
Chart: Time (days)
Unused catalyst with variation in temperature:
Long-term test after 2 weeks of testing:
 Nitridation of catalyst increases the activity
615°C
615°C
515°C
515°C
515°C
0.1%

## Slide 16: Present perspective Future perspectives
Testing catalysts at higher pressure for implementation in Aspen model
Understanding of the mechanism on the non-noble metal catalyst
Development of highly active & stable non-noble metal catalysts

## Slide 17: 2. Plasma reactor

## Slide 18: Plasma reactors for NH3 cracking
Reactor | Gliding arc plasmatron (GAP) | Pin-to-pin arc discharge (P2P)
Feed flow rate | 10 – 20 Ln/min | 10 – 20 Ln/min
Plasma power | 255 – 890 W | 115 – 445 W
Achieved HyPACT conversion | 99 % | 94 %
 | Best plasma reactor selected after 1st year of HyPACT | New plasma reactor Simpler design with easier heat recovery
4 different reactors were thoroughly evaluated [1]
2 most promising:
[1] Igor Fedirchyk, Ivan Tsonev, Rubén Quiroz Marnef and Annemie Bogaerts, “Plasma-assisted NH3 cracking in warm plasma reactors for green H2 production”, Chemical Engineering Journal, vol. 499, p. 155946, doi: 10.1016/j.cej.2024.155946.

## Slide 19: New plasma reactor for NH3 cracking: P2P arc
P2P: measured plasma temperature is ~ 3700 ⁰C
P2P: 30 % more efficient than GAP with 100 % NH3 feed
Best performing reactor among those tested for HyPACT
Ref: Igor Fedirchyk, Ivan Tsonev, Rubén Quiroz Marnef and Annemie Bogaerts, “Plasma-assisted NH3 cracking in warm plasma reactors for green H2 production”, Chemical Engineering Journal, vol. 499, p. 155946, doi: 10.1016/j.cej.2024.155946.

## Slide 20: Comparison with state of the art
HyPACT reactors are among the best performing plasma reactors for NH3 cracking
P2P: lowest EC among known plasma reactors when cracking 100 % NH3 feed: 120 kJ/mol
Figure adapted from: Igor Fedirchyk, Ivan Tsonev, Rubén Quiroz Marnef and Annemie Bogaerts, “Plasma-assisted NH3 cracking in warm plasma reactors for green H2 production”, Chemical Engineering Journal, vol. 499, p. 155946, doi: 10.1016/j.cej.2024.155946.

## Slide 21: Plasma reactors: P2P vs GAP conversion @ target EC
EC HyPACT target (56 kJ/mol) was achieved for all feed compositions
P2P arc reactor provides 1 % higher total NH3 conversion in HyPACT for the feeds with higher concentration of NH3 (8 % and 10 %) → 5-10 % improvement over GAP reactor
To reach target NH3 conversion in HyPACT (98 %) we must double conversion in plasma
Can be done by resolving the main issue: part of NH3 feed passes reactor without contact with plasma

## Slide 22: Plasma modelling: efficient operating conditions
Thermal ammonia cracking is a very slow process
Plasma decreases conversion time
Non-thermal plasma (= electron-induced chemistry): high EC
Warm plasma: fast + lower EC (120 kJ/mol), cf. slide 20
Plasma chemistry: many reactions ⇒ Complex chemistry set
Computer simulations allow for understanding and improvement
Ideal operating regime!
Ref: "Modeling insights for plasma chemical kinetics in warm plasma NH3 cracking", Seunghwan Bang, Stein Maerivoet, François Reniers and Annemie Bogaerts, submitted to Green Chemistry Journal

## Slide 23: Plasma modelling: P2P reactor
Flow profile around ceramic holder for electrode pin
Temperature profile
High-voltage
Electrode
Ground
Electrode
Initial strong vortex flow
Steadily decays into laminar flow over 150 mm
5600 °C plasma arc
Surrounded by cold unreacted gas
Glowing electrode
Ref: "Spatially resolved modelling of NH3 cracking in warm plasma ", Rubén Quiroz Marnef, Stein Maerivoet, Ivan Tsonev, François Reniers and Annemie Bogaerts, submitted to Chemical Engineering Journal

## Slide 24: Plasma modelling: model vs experiment
Thermal model captures main experimental trends
NH3 conversion is efficiently driven by thermal chemistry
Specific Energy Input = Power/Flow Rate
Ref: "Spatially resolved modelling of NH3 cracking in warm plasma ", Rubén Quiroz Marnef, Stein Maerivoet, Ivan Tsonev, François Reniers and Annemie Bogaerts, submitted to Chemical Engineering Journal

## Slide 25: 3. Thermal swing adsorption

## Slide 26: Design of an adsorption-based purification step
Main goals
  PEM Fuel cell quality H2 stream: < 0,100 ppb to avoid cell electrodes poisoning
  In full heat integration: make use of the thermal heat (plasma & thermocatalytic steps) available for the regeneration cycle
  Recover the residual ammonia and send back to the cracker
  Using commercially availables zeolites
Methodology
  Screening of zeolites for optimal NH3 sorption (equilibrium & usable)
  Experimental characterization of the isotherms
  Experimental characterization of the breakthrough curves
Design of a Temperature Swing Adsorber (TSA)

## Slide 27: Material screening: Equilibrium & dynamic loading (D3.2.1)
Mole sieves (3-5A, 13X) & Y-zeolites (CBV40-760, including pelletized)
  Pressure between 0,1 & 2,5 bar; Temperature between 10 & 50 °C
Notes: Isosteric heat 11 – 20 kJ/mol
Isotherm modem less than 2% deviation

## Slide 28: TSA design from dynamic loading experiments
Convection-dispersion model (NH3 adsorption)
  Effective axial dispersion from step change from an inert gas tracer (He)
From inert tracer experiments
Effect of the setup PLUS the QMS
Effective axial dispersion (Dz)
Superficial gas velocity (u)
Normalized breakthrough function

## Slide 29: Mechanical design of the TSA system

## Slide 30: Mechanical design of the TSA system (D3.3.1)
Preliminary view
  Without thermal insulation
  Gas preheating not visible
Four 10 mmID, 20 cm long columns
  5 Nl/min: 1% NH3 to 0,1 ppb
  Up to 10 g of sorbent
  12-25 min adsorption cycles
System delivery:
  December 12, 2024
Fully enclosed & connected to HVAC (ammonia & H2…)
  WDH: 2,5 m  0,7 m  1,7 m
SOP in preparation

## Slide 31: 4. Process simulation

## Slide 32
Refining and actualization of the Aspen model
based on experimental data
Total conversion = 98.2%
Ref: Frea Van Steenweghen, Annabel Veschueren, Igor Fedirchyk, Johan A. Martens*, Annemie Bogaerts, and Lander Hollevoet, “Reversed Plasma Catalysis Process Design for Efficient Ammonia Decomposition”, ACS Sustainable Chemistry & Engineering, vol. 13 (2), p. 737-743, DOI: 10.1021/acssuschemeng.4c08899

## Slide 33
Refining and actualization of the model
based on experimental data
Chart: Energy kJ.molNH3-1
| Energy need | Energy recovery | Net energy consumption
 | 134.1552
Heat from compressor | 29.0107
Heat from plasma | 51.1338

Compression | 30.8264 | 30.8264
Plasma reactor | 105.1445 | 105.1445
Catalytic reaction | 42.7936
Heating of feed | 13.7448 | 0
Evaporation | 23.6061
Ref: Frea Van Steenweghen, Annabel Veschueren, Igor Fedirchyk, Johan A. Martens*, Annemie Bogaerts, and Lander Hollevoet, “Reversed Plasma Catalysis Process Design for Efficient Ammonia Decomposition”, ACS Sustainable Chemistry & Engineering, vol. 13 (2), p. 737-743, DOI: 10.1021/acssuschemeng.4c08899

## Slide 34
Exploring alternative process configurations
Our process
Comparison with Plasma catalysis
at same conditions & same catalyst/plasma type
Lab experiments
& Aspen simulation
 | Plasma catalysis (post-plasma) | Reversed plasma catalysis
NH3 conversion | 98.2% | 98.2%
Treactor [°C] | 410 | 410
Preactor [bar] | 1 | 1
Pproduct [bar] | 50 | 50
Energy use [kJ.molNH3-1] | 128 | 136
Exergy use [kJ.molNH3-1] | 60.4 | 60.5
Catalyst need [gcat.h.molNH3-1] | 8.8 | 3.9
Ref: Frea Van Steenweghen, Annabel Veschueren, Igor Fedirchyk, Johan A. Martens*, Annemie Bogaerts, and Lander Hollevoet, “Reversed Plasma Catalysis Process Design for Efficient Ammonia Decomposition”, ACS Sustainable Chemistry & Engineering, vol. 13 (2), p. 737-743, DOI: 10.1021/acssuschemeng.4c08899

## Slide 35
Comparison with other process configurations
Single GAP plasma does not reach 98% conversion
3x more catalyst needed for single thermocatalysis
Single reactor configurations: catalysis & plasma
For reaching 98.2% conversion with same catalyst/plasma type
Chart: Net energy / exergy consumption (kJ.molNH3-1)
| Thermo- catalysis | Reversed plasma catalysis
net exergy consumption (kJ/mol NH3 conv) | 43.357 | 57.4989
net energy consumption (kJ/mol NH3 conv) | 34.8548 | 78.472
Catalyst need (W/F) | 10.5786 | 3.8696
Net energy consumption
Net exergy consumption
Catalyst use
Ref: Frea Van Steenweghen, Annabel Veschueren, Igor Fedirchyk, Johan A. Martens*, Annemie Bogaerts, and Lander Hollevoet, “Reversed Plasma Catalysis Process Design for Efficient Ammonia Decomposition”, ACS Sustainable Chemistry & Engineering, vol. 13 (2), p. 737-743, DOI: 10.1021/acssuschemeng.4c08899

## Slide 36: Theoretical vs experimental energy cost
Chart: Net energy consumption kJ.molNH3-1
| Experimental | Theoretical (1 bar) | Theoretical (5.5 bar)
EC (kJ.molNH3-1) | 135.9709 | 85 | 71
Improvement of plasma efficiency
Increasing operating pressure
Future perspectives
Implementation of non-noble metal catalyst
Implementation of data at higher operating pressure

## Slide 37: 5. Virtual lab scale demonstration

## Slide 38
Integration of the TSA model in Process model
Integration of the TSA in the overall process model
  TSA model using Aspen Adsorption
Aspen Adsorption model
  Increasing level of complexity
    From validation in a simple system (IN+BED+OUT, breakthrough)
30 Nml/min, 20% NH3; 1,05 g
30 Nml/min, 20% NH3; 1,05 g
No axial dispersion

## Slide 39
Numerical design of TSA model in the process model
To full cycling operation of the virtual TSA (2-20 Nl/min):
  5 Nl/min @ 1% NH3  0,1 ppb (110-7 mol/mol)
  Convection & pressure drop, adiabatic operation (gas & solid conduction), all properties constant
Cycle design
    1 - Adsorption cycle
      1 bar, 30 °C, maintain yNH3 below 0,1 ppb
    2 – Heating
      From 30 to 350 °C for the regeneration
      Under pure hot ammonia
    3 – Cooling
      Back to 30 °C using an inert

## Slide 40
Numerical design of TSA model in the process model
Cycle duration
    1 - Adsorption cycle
      yNH3 > 0,1 ppb @ t > 18,5 min  18 min
    2 – Heating
      Using heated ammonia
    3 – Cooling
      Using an inert gas

## Slide 41
Numerical design of TSA model in the process model
Cycle duration
    1 - Adsorption cycle
      yNH3 > 0,1 ppb for 18 min
    2 – Heating
      Temperature reaches 350 °C @ t  20 min
      Ammonia flowrate returns to set point@ t = 19,7 min
      2 min
    3 – Cooling
      Using an inert gas

## Slide 42
Numerical design of TSA model in the process model
Cycle duration
    1 - Adsorption cycle
      yNH3 > 0,1 ppb for 18 min
    2 – Heating
      Regeneration for 2 min
    3 – Cooling
      Back to using an inert
      Ammonia mole fraction to 1% in less than 1 min
      Cooling in 3,3 min @ t = 1400 s (23,3 min)
      4 min

## Slide 43
Further optimizing
Refine the simulation & experimental validation
  Numerical aspects, addition of valves & instruments, thermal insulation
Simulate the continuous 1-20 Nl/min setup
  Adsorption is the critical part
  6 columns, 30% sorbent loading

## Slide 44: Testing heating and cooling cycles
Qreg

## Slide 45: Testing flow and VICI valve activation-Step 1: Column 1 in adsorption and column 3 in regeneration mode.
Valves 2-4 Position A
Valves 1-3 Position A

## Slide 46: Testing flow and VICI valve activation-Step 3: Column 3 in adsorption and column 1 in regeneration mode.
Valves 1-3 Position B
Valves 2-4 Position A
The same procedure applies to steps 2 and 4.

## Slide 47: Leak detection and repair

## Slide 48: Benchmarking & analysis NH3 downstream applications

## Slide 49
Technical readiness level (TRL) of HyPACT project
Lab-scale experimental demonstration of each component
Virtual demonstration by simulation model
End TRL = 3-4

## Slide 50: Alternative cracking technologies
Type |  | Total energy consumption | Total energy recovery | Net energy consumption | Material cost
HyPACT Thermo-catalytic + plasma | Simulation |  |  |  | 
 | Experimental |  |  |  | 
Thermo-catalytic | Noble catalysts |  |  |  | 
 | Non-noble catalysts |  |  |  | 
Plasma | Cold plasma literature |  |  |  | 
 | Warm plasma Experimental |  |  |  | 
Electrolysis | literature |  |  |  | 
Good
Bad
Notes: In this figure the energy consumption of the HyPACT process is compared to the state of the art ammonia cracking thermo-catalytic cracking), plasma cracking and ammonia electrolysis. As can be seen, the latter two consume much more energy than thermo-catalytic cracking and the HyPACT process. For plasma, this is because cold plasmas require a lot of energy and the technology of warm plasmas is not yet enough advanced. For electrolysis, the efficiency of the process is very low resulting in a larger amount of energy.
In literature, ruthenium is often proposed as the best catalyst for thermo-catalytic cracking. However, ruthenium is very expensive, hence the red color for material cost for thermo-catalytic cracking. This is however not necessary as has been showed here in HyPACT that less expensive catalysts also perform well enough.

## Slide 51: Energy applications of ammonia: Maritime
Notes: Several ammonia powered vessels are in developing. At the top left we see the Viking Energy from Eidesvik with an ammonia powered engine built by Wärtsilä ready to set sail in 2026. Top right is the Yara Ede by CMB.Tech, Delphis and with support of the NCL (Yara will provide ammonia) also ready by 2026. Bottom left a ship by Exmar and WinGD ready also by 2026. And bottom left we have dual fuel diesel-ammonia powered vessel which already sailed around in Signapore.

## Slide 52: Energy applications of ammonia: Power generation
Notes: IHI corporation built a cofiring ammonia pilot powerplant and started testing in 2024.

## Slide 53: Cracking technology demonstrations
Company | Technology | What
Air Liquide | Thermo-catalytic | Pilot reactor
Topsoe | Thermo-catalytic | Industrial cracker 2 X 2400 MTPD
Duiker Clean Technologies | Thermo-catalytic | SCO  cracking  purify
Amogy | Thermo-catalytic | 200kW – 400kW powerpack
H2Site | Thermo-catalytic + membrane | onboard cracker for electricity
… |  | 
Notes: Several companies have already tested and demonstrated ammonia cracking technologies. Click on the links in the right column to find out more.
Amogy cracks ammonia on board with thermo-catalytic  then adsorber module to purify hydrogen  fuel cell all in the powerpack
H2Site  onboard cracker for electricity for auxiliary consumption
Duiker  S(toichiometry) C(ontrolled) O(xidation) = combustionsystem which destroys ammonia with low NOx formation
MTPD = metric tonnes per day

## Slide 54: Future valorization of HyPACT project

## Slide 55: The research successes
Precious metal-free catalysts:
  Performance ~ State-of-the-art Ru-catalyst NH3 conversion > 90% at 500°C
  Stable over > 50 h
Novel warm plasma reactors for NH3 cracking:
  Performance > literature plasma reactors Energy cost of 120 kJ.mol-1 (for 100% NH3 feed)
Developed state-of-the-art plasma model with plans for improved reactor design
Zeolite-based H2 purification
  by simulating moving bed
  With recirculation of NH3
Competitive net energy consumption due to smart heat integration
Low material & installation cost
Compatible with renewable energy

## Slide 56: One approach of HyPACT NH3 cracking technology use
Large-scale Haber-Bosch NH3 synthesis
(Pure NH3 @-33°C)
Transported in vessels via ship
At harbors:
Large-scale cracking of NH3
Hydrogen product
Transported via pipelines / trucks / …
Large-scale HyPACT technology use

## Slide 57
Stijn Meel
Stijn.Meel@waterstofnet.eu